## Slide 1
PRR of the PSD MPPC irradiation study
Sergey Morozov
on behalf of the PSD team

## Slide 2
PSD module scintillators assembly
Scintillator tiles
WLS fibers
Lead
- 60 Pb (16mm) + Scint (4mm) samples, length of the module ~ 5.6 λint
- light collection: 6 WLS fibers from 6 sequentially scint. tiles are combined
into one optical connector at the end of module
- light detection: SiPMs mounted on the back side of the PSD calorimeter
- high neutron background is expected → only SiPMs are used at the PSD, all
FEE will be separated and installed in the radiation safe place
photodetectors
Light readout of the PSD modules with SiPMs
SiPM performance in irradiation conditions has been studied in LAB and on beam
<номер>

## Slide 3
<номер>
PSD photodetectors
Requirements
- high dynamic range for linear response for small (MIP) and large (ion hadron showers) signals (Npix)
- small recovery time (we have fast signals at high rates)
- radiation hardness
Radiation hardness has been tested with a help of the cyclotron of NPI (Řež) with a "white" (from thermal
up to 35 MeV) and mono-energetic (22 MeV) neutron spectra: irradiation fluxes 4x1010 – 6x1012 n/cm2
the best variant
-3010PS

## Slide 4
<номер>
Dark current vs over-voltage for different SiPMs dependence of irradiation dose
Dark current measured as a function of forwarding bias voltage for different SiPMs before and after irradiation with 1 MeV equivalent neutron fluence.
Hamamatsu MPPC shows the moderate increase of dark current after irradiation

## Slide 5
<номер>
SiPM response to illumination by UV LED measured as a function of over-voltage for Hamamatsu MPPC S12572-010P in linear scale before and after irradiation with different 1 MeV equivalent neutron fluence. (left) presents a full scale, (right) is magnified for highly irradiated SiPMs.
Conclusion: the signal has a significant drop after the radiation dose about 2*1012 which is 20 times more then expected dose at the PSD. The signal level can be restored with HV adjustment.
LAB tests with LED light flashes. Signal vs over-voltage for different SiPMs irradiation doses.

## Slide 6
<номер>
signal-to-noise ratio (left) and signal resolution (right) measured as a function of over-voltage for Hamamatsu MPPC S12572-010P before and after irradiation with different 1 MeV equivalent neutron fluence.
Conclusion: the signal-to-noise ration will be changed only about 10 times at PSD expected radiation dose (about 1011).
LAB tests with LED light flashes. Resolution vs over-voltage for different SiPMs irradiation doses.

## Slide 7
The best SiPMs for light detection
Hamamatsu S14160-3010P
Sensitive area - 3 x 3 mm2
Number of pixels - 90 000
nominal gain - 1 x 105,
Gain ~1% /1ᵒC
Pixel recovery time - 10 ns
PDE -18%
.
PSD photodetectors
<номер>
NIEL is on acceptable level.
from Anna Senger,
CBM Collaboration
meeting, March 2021
Au+Au
Non Ionizing energy losses (NIEL)

## Slide 8
<номер>
Conclusions of laboratory tests with irradiated SiPMs:
- Hamamatsu SiPM was found to fit the CBM PSD general requirements at least up to an accumulated
fluence of 2.5 × 1011 neq/cm2, which corresponds to 1 year of CBM operation at 1 MHz collision rate
- Dark current increased in the operation range from 0.5 up to 3 V, which is near the limit that current
power supply boards can deliver – will be taken into account in FEE design
- Signal response to LED illumination decreased by 50%, which can be fixed during the detector operation
by the adjustment of the overvoltage and/or readout chain recalibration
- Signal-to-noise ratio for SiPMs irradiated by 2.5 × 1011 neq/cm2 decreased by an order of
magnitude. Then the shortening of dynamic range can be compensate with the adjustment of the
over-voltage.

## Slide 9
PSD photodetectors – SiPMs
PSD performance with
irradiated SiPMs
(beam tests at CERN)
<номер>

## Slide 10
Energy distributions for muons selected for the cross calibration of all the 10 sections
measured with SiPMs irradiated by 2.5 × 1011 neq/cm2.
<номер>
We can still see the MIP signals!
Hamamatsu MPPCs
S12572-010P
SiPM performance: MIP signals after irradiation

## Slide 11
Change of the PSD module energy resolution at low energies, after SiPM irradiation with different n fluences. The change in the energy resolution of the PSD module equipped with irradiated SiPMs. One can see that there is only very minor decrease in σE/E after irradiation by 2.5×1011 neq/cm2, and fitted value is about 70 %/√ E (GeV) in case of for both irradiated and non-irradiated SiPMs.
<номер>
Hamamatsu MPPCs
S12572-010P
SiPM performance: PSD energy resolution

## Slide 12
Energy resolutions for proton beams of different energies estimated with different amplitude cuts used for noise suppression. All the investigated SiPM batches irradiated with different fluences are presented.
<номер>
Hamamatsu MPPCs
S12572-010P

## Slide 13
Change of the PSD module energy resolution at both low and high energies after SiPM irradiation by 2.5 × 1011 neq/cm2.
<номер>

## Slide 14
Change of the PSD module energy resolution after SiPM irradiation as a function of 1 MeV equivalent neutron fluence achieved by SiPMs, measured with proton beams of different energies.
Linearity of the PSD module response to proton beams in momentum range of 2 – 80 GeV/c before and after SiPM irradiation with different fluences.
<номер>

## Slide 15
<номер>
Conclusions of CERN beam tests with irradiated SiPMs:
- PSD module energy resolution changed only slightly in case of light readout with SiPMs irradiated
by 2.5 × 1011 neq/cm2. This corresponds to SiPMs located closest to the beam hole after a year of
CBM operation at 1 MHz collision rate (assumed to be 2 months of an uninterrupted running)
- Despite the increased noise level, the possibility of the calibration with minimum ionizing particles
was proven for SiPMs irradiated by 2.5 × 1011 neq/cm2.
- The energy linearity remained consistent for irradiated SiPMs with data measured with non-irradiated SiPMs.
- The energy resolution of PSD remains unchanged up to irradiation fluences of 2.5 × 1011 neq/cm2
MPPC S14160-3010P have
been ordered for whole PSD

## Slide 16
BACKUP
<номер>

## Slide 17
<номер>
Comparison of signal response to LED (top left), noise (top right), signal-to-noise ratio (bottom left) and resolution (bottom left) for Hamamatsu MPPC S12572-010P, Hamamatsu MPPC S14160-3010PS and Ketek PM3315-WB-A0 as a function of over-voltage before and after irradiation with 2.5 × 1011 neq/cm2.

## Slide 18
Change of the PSD module energy resolution at both low and high energies after SiPM irradiation with different fluences.
<номер>